## Slide 1
Javier Junquera
How to compute the
Born effective charge tensor

## Slide 2
Definition of the Born effective charges, also known as dynamical charges
Units: electron charges
For periodic solids, the Born effective charge of atom is a tensor defined as the coefficient of proportionality at the linear order and under the condition of zero macroscopic electric field, between the macroscopic polarization per unit cell created in direction and a cooperative displacements of atoms in direction
Read pages 106 and following of Philippe Ghosez’s PhD thesis
http://www.phythema.ulg.ac.be/webroot/misc/books/PhD-Ph.Ghosez.pdf

## Slide 3
In SIESTA computed from finite differences of the bulk spontaneous polarization
SrTiO3 in the centrosymmetric bulk cubic structure
To compute the phonons, the atomic masses are introduced in this block
We are going to displace all the atoms in the unit cell 0.01 Bohrs along the x, y, and z direction
For each atomic configuration, we compute the macroscopic polarization with this Polarization Grid in reciprocal space

## Slide 4
Born effective charges dumped into a file: SystemLabel.BC
x y z
x 2.5227042 0.0000000 0.0000000 |
y 0.0000000 2.5227042 0.0000000 | Born effective charges for Ba
z 0.0000000 0.0000000 2.5227043 |
--------------------------------------------------
x 7.5522144 0.0000000 0.0000000 |
y 0.0000000 7.5522144 0.0000000 | Born effective charges for Ti
z 0.0000000 0.0000000 7.5522132 |
--------------------------------------------------
x -2.0647380 0.0000000 0.0000000 |
y 0.0000000 -2.0647380 0.0000000 | Born effective charges for O1
z 0.0000000 0.0000000 -5.9514365 |
--------------------------------------------------
x -2.0647380 0.0000000 0.0000000 |
y 0.0000000 -5.9514365 0.0000000 | Born effective charges for O2
z 0.0000000 0.0000000 -2.0647380 |
--------------------------------------------------
x -5.9514365 0.0000000 0.0000000 |
y 0.0000000 -2.0647380 0.0000000 | Born effective charges for O3
z 0.0000000 0.0000000 -2.0647380 |
--------------------------------------------------

## Slide 5
Acoustic sum rule
It is important that the acoustic sum rule is preserved by the Born effective charges
(if we displace the whole solid rigidly, no polarization should be generated)
In our simulation, taking , and rounding to the third significant digit
Substracting this same amount to all the atoms
To fulfill the acoustic sum rule, we divide the sum by the number of atoms
2.523 + 7.552 -2.065 -2.065 -5.951 = -0.006
2.524 + 7.553 - 2.064 - 2.064 - 5.949 = 0
-0.006/ 5 = -0.0012

## Slide 6
Comparison with previous results
First-principles studies of ferroelectric oxides
K. M. Rabe and Ph. Ghosez, included in
Physics of Ferroelectrics. A Modern Perspective.
Topics in Applied Physics
K. Rabe, Ch. Ahn, and J. –M. Triscone (Editors)
Springer-Verlag, Heidelberg (2007)
Adapted from
Ph. Ghosez et al. ,
Phys. Rev. B 58, 6224 (1998)

## Slide 7
Phonon frequencies and eigenvectors at the Γ-point
Three frequencies are zero,
They correspond to translational modes
- Go to the directory
$cd <your_siesta_path>/Util/Vibra/Src
To compile the vibra suite with the same arch.make as in siesta, type
$make
Go back to the directory where you are running the exercise and type
$ <your_siesta_path>/Util/Vibra/Src/vibra < SrTiO3.fdf
You get the file SrTiO3.bands with the eigenvalues
and SrTiO3.vectors with the eigenvectors