## Slide 1
First-principles simulations on
PbTiO3/SrTiO3 superlattices
Javier Junquera
Pablo Aguado-Puente
Pablo García-Fernández

## Slide 2
Multitude of fascinating and exotic properties boasted by transition metal oxides
ABO3 perovskites oxides:
simple structure, wide variety of properties

## Slide 3
Some surprises at the interfaces between two oxides
E. Bousquet et al., Nature 452, 732 (2008)
Appearance of improper ferroelectricity in PbTiO3/SrTiO3 superlattices
A. Ohtomo and H. Y. Hwang, Nature 427, 423 (2004)
The interface between two good insulators (e.g. LaAlO3 and SrTiO3) is metallic

## Slide 4
Many instabilities might be present in bulk ABO3 perovskites: They often compete and tend to suppress each other
“ideal” cubic perovskite structure, taken as the high-symmetry reference configuration
Ph. Ghosez et al., Phys. Rev. B 60, 836 (1999)
Phonon dispersion curves at the bulk cubic experimental lattice constant
Signature of the instability:
a branch in the phonon dispersion curve with imaginary frequency
Stable only within a narrow range of ionic radii.

## Slide 5
Ph. Ghosez et al., Phys. Rev. B 60, 836 (1999)
G-point
(0.0, 0.0, 0.0)
Ferroelectric (FE)
R-point
(0.5, 0.5, 0.5)
Antiferrodistortive (AFD)
M-point
(0.5, 0.5, 0.0)
Antiferrodistortive (AFD)
X-point
(0.5, 0.0, 0.0)
Antiferroelectric (AFE)
Typical crystal instabilities
PbTiO3 phonon dispersion curves at the bulk cubic experimental lattice constant

## Slide 6: The competition between all the structural instabilities might be altered at surfaces/interfaces
A. Munkholm et al., Phys. Rev. Lett. 88, 016101 (2002)
C. Bungaro and K. M. Rabe, Phys. Rev. B 71, 035420 (2005)
(001) PbTiO3
c(2×2) reconstructions in PbO-terminated
  Substantial enhancement of the AFD distorsion
  Driving force: shorter PbO bonds
  
  Not observed neither in TiO2 termination nor BaTiO3 surface
Top
Lateral
Surface might induced reconstructions to saturate dangling bonds

## Slide 7: PbTiO3/SrTiO3 superlattice: polarization, c/a, and phase transition T can be monitored with PTO volume
M. Dawber et al., Phys. Rev. Lett. 95, 177601 (2005)
M. Dawber et al., Adv. Mater. 19, 4153 (2007)
Tetragonality
(related with P due to the large polarization-strain coupling in PbTiO3)
Phase transition temperature
In the experiment, the number of layers of SrTiO3, ns, was fixed to 3
For PbTiO3 layers thickness larger than 3, np/ns > 1, the polarization is found to be reduded (depolarizing field effect)
For PbTiO3 layer thickness smaller than 3, np/ns<1,unexpected recovery of ferroelectricity that can not be accounted for by simple electrostatic arguments

## Slide 8: Short-period PbTiO3/SrTiO3 superlattices: the GS involves trilinear coupling between two AFD modes and a polar FE mode
E. Bousquet et al., Nature 452, 732 (2008)
In-phase AFD rotations of O octahedra
Out-of-phase AFD rotations of O octahedra
Ferroelectric mode
Improper ferroelectricity

## Slide 9: Interesting and useful features of improper ferroelectrics
E. Bousquet et al., Nature 452, 732 (2008)
High and T-independent 
High Pz T=0
Normal sample
(9/3)
Anomalous sample
(2/3)
N. Sai et al., Phys. Rev. Lett. 102, 107601 (2010)
Reduced sensitive to depolarizing fields
The instability to a single domain ferroelectric state does not vanish even when depolarizing field remains unscreened
Ps (YMnO3 thin films) ≈ Ps(YMnO3 bulk)
Promising way of generating novel magnetoelectric couplings
N. A. Benedek and C. J. Fennie, Phys. Rev. Lett. 106, 107204 (2011)
Possible paths for electric-field switching of magnetization in Ca3Mn2O7

## Slide 10: First-principles study on PbTiO3/SrTiO3 superlattices
Influence of the epitaxial strain
Eventual stabilization of domains

## Slide 11: First-principles study on PbTiO3/SrTiO3 superlattices
Influence of the epitaxial strain
Eventual stabilization of domains

## Slide 12
Many oxides have similar lattice constants allowing for a good match at the interfaces
D. G. Schlom et al., Annu. Rev. Mater. Res. 37, 589 (2007)
What would happen if we could mix materials with different properties?
Potential for novel behaviour
Current interest in functional oxides is largely based on engineered epitaxial thin films

## Slide 13: First-principles simulations on monodomain PbTiO3/SrTiO3 superlattices
Oxygen octahedra labeled according to:
- chemical identity of first two
neighbours layers
- polarization
(2/2) superlattice
Local Density Approximation (LDA)
(2 × 2) in-plane periodicity to allow for TiO6 octahedra rotations and tiltings
Mechanical boundary conditions implicitly treated by fixing the in-plane lattice constant
Short-circuit electrical boundary conditio

## Slide 14: First-principles atomic relaxations on monodomain PbTiO3/SrTiO3 superlattices
(2/2) superlattice
Step 1:
Getting a reference non-polar structure
Relaxation of the atomic position and lattice vectors
BUT
With some constraints to avoid the appearance of a polarization

## Slide 15: First-principles atomic relaxations on monodomain PbTiO3/SrTiO3 superlattices
(2/2) superlattice
Step 2:
Getting the most stable phases
Starting from the most stable non-polar phase,
SYMMETRY IS BROKEN
A new atomic relaxation is performed

## Slide 16: Polarization-strain coupling in monodomain PbTiO3/SrTiO3 (2/2) superlattices
Common cubic substrates
For tensile strains:
-polarization lies along [110] direction
(aa-phase)
-no electrostatic restriction to keep the in-plane polarization at the same value
For intermediate regime:
-continuous rotation of polarization
(r-phase)
-second order phase transitions
Strain (%)
For compressive strains:
-homogeneous polarization stabilized along z (c-phase)
preserved at the PbTiO3/SrTiO3 interface
(electrostatic restriction)
PW: SrTiO3 lattice constant using plane wave
3.84 Å
NAO: SrTiO3 lattice constant using numerical atomic orbitals (3.87 Å)

## Slide 17: Large electromechanical response in monodomain PbTiO3/SrTiO3 (2/2) superlattices
Polarization as a function of stress
d13
d11STO
d11PTO
Piezoelectric components diverge in a region very accesible experimentally, around lattice constant of SrTiO3

## Slide 18: FE-AFD-strain coupling in monodomain PbTiO3/SrTiO3 (2/2) superlattices
Common cubic substrates
Compressive strains favour rotation of the TiO6 octahedra
Tensile strains favour tilting of the TiO6 octahedra
J. Rondinelli and N. A. Spaldin, cond-mat/1103.4418
* : rotations x : tiltings

## Slide 19: Behaviour of the different TiO6 octahedra explained by a covalent model
TiO2 layer and Pb atoms below
When a large compressive strains are applied, P+ rotates more than P-.
When Pb atom moves up (FE),
O moves towards it to form stronger covalent bonds
Reinforcement of the P+ TiO6 rotation

## Slide 20: Behaviour of the different TiO6 octahedra explained by a covalent model
TiO2 layer and Pb atoms below
When a large compressive strains are applied, P+ rotates more than P-.
When Pb atom moves up (FE),
O moves towards it to form stronger covalent bonds
Reinforcement of the P+ TiO6 rotation
TiO2 layer and Pb atom up
When Pb atom moves up (FE) all Pb-O bonds are weakened
Reduction of the P- TiO6 rotation
* : rotations x : tiltings

## Slide 21: Monodomain PbTiO3/SrTiO3 superlattices with different periodicities
Independently of the periodicity: the ground state
- always in-plane and out-of-plane polarization
(although for n=1, essentially degenerated with the [001] configuration
found in E. Bousquet et al. 452, 732 Nature (2008)
- n ≥ 2, pointing along the diagonal of the perovskite unit cell in PbTiO3
In-plane lattice constant: theoretical SrTiO3 (3.874 Å)
Reason for the stabilization of the [111] phase:
PbTiO3 likes rotate more than a monotomic decrease of

## Slide 22: First-principles study on PbTiO3/SrTiO3 superlattices
Influence of the epitaxial strain
Eventual stabilization of domains

## Slide 23
Structural and dielectric properties of PTO/STO superlattices as a function of the periodicity, electrodes and electric fields
Tune properties by changing periodicity, electrodes, …
Close competition between mono and polydomain ground state
Ideal system for the study of nanodomains under applied electric fields using x-ray diffraction
Nb-doped SrTiO3/…/PbTiO3/SrTiO3/…/Au
SrRuO3/…/PbTiO3/SrTiO3/…/SrRuO3
Remnant polarization as a function of the PbTiO3 volume fraction
Follows DGL theory (assumes mono)
Does not follow DGL theory
Almost 0 remnant polarization except for the highest PbTiO3 volume fractions
Structural parameters almost identical for the two series
P. Zubko et al., Phys. Rev. Lett. 104, 187601 (2010)
Motivation: study of domains in PbTiO3/SrTiO3 superlattices from first-principles
Suggest of a polydomain phase with domain wall motion

## Slide 24
180° domain structures detected and characterized in PbTiO3 thin films grown on SrTiO3(001) substrates
Real space AFM image
Phase diagram
Satellites around PbTiO3 Bragg peaks in synchrotron x-ray
C. Thompson et al., Appl. Phys. Lett. 93, 182901 (2008)
D. D. Fong et al., Science 304, 1650 (2004)
Fa, Fb : domain phases with different periodicities
Fg : monodomain phase
P : paraelectric

## Slide 25
(3,3) superlattice → 30 atoms
Nx x Ny supercell → Impose lateral size of domains
Ny allows to switch on (Ny =2) and off (Ny = 1) Oxygen octahedra rotations
Example: 6x1 supercell
Simulation of domains in PbTiO3/SrTiO3 superlattices building of the supercell

## Slide 26
Simulation of domains in PbTiO3/SrTiO3 superlattices building of the supercell
(3,3) superlattice → 30 atoms
Nx x Ny supercell → Impose lateral size of domains
Ny allows to switch on (Ny =2) and off (Ny = 1) Oxygen octahedra rotations
Example: 6x1 supercell

## Slide 27
Domains in PbTiO3/SrTiO3 (3/3) superlattices: Energetics
The energy of the polydomain structure decreases with the increase of the domain periodicity (minimum found around Nx =12)
AFD not allowed
AFD allowed
Domain walls along [110]
For a given domain periodicity, the energy is lowered if the AFD distortions are allowed
(Importance of FE-AFD coupling)
22 meV
10 meV

## Slide 28
Domains in PbTiO3/SrTiO3 (3/3) superlattices: Energetics
The energy of the polydomain structure decreases with the increase of the domain periodicity (minimum found around Nx =12)
AFD not allowed
AFD allowed
Domain walls along [110]
For a given domain periodicity, the energy is lowered if the AFD distortions are allowed
(Importance of FE-AFD coupling)
The effect of the domain wall orientation is small
The most stable phase: monodomain
BUT
Difference in energy with respect the most stable polydomain phase small.
Both phases might compete.
9 meV

## Slide 29
(3,3) superlattice
6 unit cells of domain periodicity
Fully relaxed
Vortices at DW
Closed by a large in-plane displacement of the Pb atoms
Domains in PbTiO3/SrTiO3 superlattices: adopt the clossure-domain structure with vortices
S. Prosandeev and L. Bellaiche, Phys. Rev. B 75, 172109 (2007)
P. Aguado-Puente and J. Junquera Phys. Rev. Lett. 100, 177601 (2008)

## Slide 30
Experimental observarion of domains of closure
C.-L. Jia et al. Science 331, 1420 (2011)
Pb(Zr0.2Ti0.8)O3/SrTiO3
BiFeO3/TbScO3
C. T. Nelson et al. Nano Lett. 11, 828 (2011)

## Slide 31
Domains in PbTiO3/SrTiO3 (3/3) superlattices: vortices in larger domain periodicities
(3,3) superlattice
12 unit cells of domain periodicity
Fully relaxed
 | w/o AFD | with AFD
PPTO (μC/cm2) | (0, 0, 62) | (0, 2, 55)
PSTO (μC/cm2) | (0, 0, 32) | (0, 0, 30)
Large in-plane displacements for the Pb ~ 0.2 Å → TEM experiment?

## Slide 32
Domains in PbTiO3/SrTiO3 superlattices: domain structure induces inhomogeneous strain
(3,3) superlattice
6 unit cells of domain periodicity
Fully relaxed
Polarization domains → good screening
Domains induce large strain gradient
aPTO up = 3.97 Å
aPTO down = 3.76 Å
Δa = 0.20 Å
 | w/o AFD | with AFD
PPTO (μC/cm2) | (0, 0, 68) | (0,26,56)
PSTO (μC/cm2) | (0, 0, 25) | (0,1,23)

## Slide 33
Conclusions
Mixed ferroelectric-antiferrodistortive-strain coupling in PbTiO3/SrTiO3 superlattices
Electrostatic and covalent origin
Large electromechanical response around the strain imposed by a SrTiO3 lattice constant
Close competition between monodomain and closure-domain structures

## Slide 34
Many thanks to
Pablo Aguado-Puente
Pablo García-Fernández
Finantial support
Computer time

## Slide 35
More info …

## Slide 36: Monodomain PbTiO3/SrTiO3 superlattices with different periodicities

## Slide 37
Origin of the r-phase: PbTiO3 prefers to rotate over a reduction of the out-of-plane-polarization
~ 80 meV
Double-well curve of bulk tetragonal PbTiO3

## Slide 38
Origin of the r-phase: PbTiO3 prefers to rotate over a reduction of the out-of-plane-polarization
~ 80 meV
Double-well curve of bulk tetragonal PbTiO3
~ 45 meV
Its actually cheaper to rotate!

## Slide 39
No polarization along x

## Slide 40
Elastic vs electrostatic interlayer coupling
Domains induce large strain gradient
Related with flexoelectricity, face where cation move towards expands.
STO is forced to distort the opposite way → elastic cost
Greater electrostatic cost
Minimization of elastic energy?
Minimization of elastic energy?

## Slide 41
Simulation of monodomain PbTiO3/SrTiO3 superlattices
Bousquet et al., Nature 452, 732 (2008)
Improper FE
Strong coupling between FE and AFD modes
Monodomain configuration
Larger periodicities → Interfacial effect
(3,3) superlattices:
Bousquet et al.
Present work

## Slide 42
Inhomogeneous distortion in SrTiO3 /PbTiO3 superlattices
Domain widths:
wSTO down = 11.68 = 3 × 3.89 Å
wPTO up = 11.92 = 3 × 3.97 Å
wPTO down = 11.32 = 3 × 3.77 Å
wSTO up = 11.56 = 3 × 3.85 Å
aSTO bulk = 3.874 Å
ΔwSTO = 0.12 Å
ΔwPTO = 0.60 Å

## Slide 43
1
3
5
7
9
11
2
4
6
8
10
12
cSTO bulk = 3.874 Å
cPTO bulk = 4.025 Å
Tetragonality in polydomain SrTiO3 /PbTiO3 superlattices
Out of plane lattice parameters:

## Slide 44
PTO/STO superlattices: relative stability of monodomain and polydomain configurations
↑Nx = -23 meV
AFD instabilities increase stability
Domain periodicity ~ 12 unit cells
(experiment ~ 11 unit cells)

## Slide 45
Inhomogeneous strain due to domain structure in PTO/STO
Polarization breaks inversion symmetry → different bonding at up and down interfaces and diffetent interfacial distance.
Flexoelectric effect? → unit cell side where cations move towards, expands.
Large flexoelectric effect observed in FE materials.
Spontaeous P induces spontaneous strain gradient.
Bursian et al., Fiz. Tv. Tela 10, 1413 (1968)
Ti
O
Δz = 3.85 Å
Δz = 3.90 Å

## Slide 46
Domains of closure recently predicted using a model hamiltonian approach
S. Prosandeev and L. Bellaiche, Phys. Rev. B 75, 172109 (2007)
48 Å thick PbZr0.4Ti0.6O3 thin films
sandwiched with a nongrounded metallic plate (top) and a non-conductive substrate (bottom)
d = 0
d = 0.5 a
d = 0.3 a
Dead layer thickness

## Slide 47
Domains of closure recently predicted using a phenomenological thermodynamic potential
G. B. Stephenson and K. R. Elder, J. Appl. Phys. 100, 051601 (2006)
Polarization distribution
Equilibrium field distribution
242 Å thick PbTiO3 thin films sandwiched with a nonconducting SrTiO3 electrodes @ 700 K stripe period 132 Å

## Slide 48
ABO3 perovskite structure exhibits several lattice instabilities. Competition between polar and non polar instabilities.
Balance might be altered in nanostructures
Mechanical
Electrostatic
Surface
Defects
(vacancies, misfit dislocations…)
Interfacial chemistry
Antiferrodistortive
Ferroelectric
Antiferroelectric

## Slide 49
Inhomogeneous strain due to domain structure in PbTiO3/SrTiO3 superlattices
Δz = 3.85 Å
Δz = 3.90 Å
Polarization breaks inversion symmetry → different bonding at up and down interfaces and diffetent interfacial distance.

## Slide 50
Elastic energy associated with inhomogeneous strain play a role in domain structure
Balance:
Elastic energy ↔ Electrostatic energy ↔ Domain wall energy
Domain wall interaction more complex than in bulk/thick films
Need for a model

## Slide 51
Common wisdom: epitaxial BaTiO3 under compressive in-plane strain stabilizes the tetragonal phase, with enhancement of Ps
c
a
aa
r
ac
p
O. Diéguez et al., Phys. Rev. B 69, 212101 (2004)
B. Lai et al., Appl. Phys. Lett. 86, 132904 (2005)
K. J. Choi et al., Science 306, 1005 (2004)
Enhancement of the remnant polarization
Yoneda et al., J. Appl. Phys. 83, 2458 (1998)
Enhancement of the transition temperature
BaTiO3/SrTiO3

## Slide 52
Simulation of monodomain PbTiO3/SrTiO3 (3/3) superlattices
Bousquet et al., Nature 452, 732 (2008)
Improper FE for the short-period superlattices
Strong coupling between FE and AFD modes
Monodomain configuration
Larger periodicities → Interfacial effect
[PbTiO3]3/[SrTiO3]3 = (3,3) superlattices:
 | Bousquet et al. | Present work
Ground state | FEz + AFDz | FEz + FExy + AFDz + AFDxy
-24 meV

## Slide 53
Simulation of monodomain PbTiO3/SrTiO3 (3/3) superlattices
Bousquet et al., Nature 452, 732 (2008)
Strong coupling between FE and AFD modes
Monodomain configuration
Larger periodicities → Interfacial effect
 | Bousquet et al. | Present work
Ground state | FEz + AFDz | FEz + FExy + AFDz + AFDxy
PSTO (μC/cm2) | (0, 0, 37.5) | (5, 5, 29)
PPTO (μC/cm2) | (0, 0, 35.8) | (36, 32, 31)
[PbTiO3]3/[SrTiO3]3 = (3,3) superlattices:
Improper FE for the short-period superlattices

## Slide 54
Simulation of monodomain PbTiO3/SrTiO3 (3/3) superlattices
Bousquet et al., Nature 452, 732 (2008)
Strong coupling between FE and AFD modes
Monodomain configuration
Larger periodicities → Interfacial effect
[PbTiO3]3/[SrTiO3]3 = (3,3) superlattices:
 | Bousquet et al. | Present work
Ground state | FEz + AFDz | FEz + FExy + AFDz + AFDxy
PSTO (μC/cm2) | (0, 0, 37.5) | (5, 5, 29)
PPTO (μC/cm2) | (0, 0, 35.8) | (36, 32, 31)
Strain of PTO on STO | -1.2% | -0.5%
FE ↔ AFD coupling is extremely sensitive to strain!
Improper FE for the short-period superlattices

## Slide 55
 | Present work
Ground state | FEz + FExy + AFDz + AFDxy
PSTO (μC/cm2) | (5, 5, 29)
PPTO (μC/cm2) | (36, 32, 31)
Simulation of monodomain PbTiO3/SrTiO3 (3/3) superlattices
[PbTiO3]3/[SrTiO3]3 = (3,3) superlattices:
~ 80 meV
~ 45 meV
Its actually cheaper to rotate!
Why PbTiO3 polarizes in-plane?

## Slide 56
Recent discoveries on transition metal oxides: one of the “top tens” scientific breakthroughs of 2007
Science, 318, 1846 (2007)

## Slide 57
The field is still in an incipient stage, comparable to that of semiconductors 60 years ago

## Slide 58
Nx=4
BaO wall
TiO2 wall
TiO2 wall
BaO wall
Nx=6
2-unit-cells thick BaTiO3 layer in between SrRuO3 electrodes
P. Aguado-Puente and J. Junquera Phys. Rev. Lett. 100, 177601 (2008)
Polydomain phases in ferrolectric nanocapacitors adopt the form of a “domain of closure”, common in ferromagnets
C. Kittel (1946)
Ferromagnetic domains

## Slide 59
P = 65 μC/cm2 → good screening
Vortices at DW ↔ Domains of closure (but in this case, closed by the displacements of the Pb atoms)
Domains of closure in PbTiO3/SrRuO3 capacitors from first-principles
SrRuO3
SrRuO3
PbTiO3
Short-circuit
4-unit-cell thick PbTiO3
6 unit cells of domain periodicity
Fully relaxed
C. Lichtensteiger et al.
“Oxide ultrathin films: science and technology”
Ed. by G. Pacchini and S. Valeri (Wiley, 2011)

## Slide 60
Domains in PbTiO3/SrTiO3 superlattices: vortices & large polarization
(3,3) superlattice
6 unit cells of domain periodicity
Fully relaxed
Vortices at DW
Polarization domains → good screening
 | w/o AFD | with AFD
PPTO (μC/cm2) | (0, 0, 68) | 
PSTO (μC/cm2) | (0, 0, 25) | 

## Slide 61
Domains in PbTiO3/SrTiO3 superlattices: vortices & large polarization
(3,3) superlattice
6 unit cells of domain periodicity
Fully relaxed
Vortices at DW
Polarization domains → good screening
 | w/o AFD | with AFD
PPTO (μC/cm2) | (0, 0, 68) | (0,26,56)
PSTO (μC/cm2) | (0, 0, 25) | (0,1,23)
-22 meV